## Slide 1: Development of Nanoscaffolds Through Oxidation on Titanium-Alloy Disks to Increase Artificial Implant Lifespan
URITC-UPRM Eisenhower Fellowship 2009
Caitlyn M. Maleck
University of Rhode Island
Mechanical Engineering Undergraduate
July 17, 2009

## Slide 2: Agenda
Introduction and Background
Methodology
Results
Preliminary Conclusions

## Slide 3: Introduction & Background
Titanium alloys commonly used in implants
Loosening of the implant can lead to future surgeries
Solution:
Objective: determine a method for creating uniform nanoscaffolds on various titanium alloys to maximize area and reduce oxide fracture

## Slide 4: Methodology
Figure 1: (Above) Samples polished with
conventional Beuhler pads up to 600 grit.
Figure 3: (Above) Tribometer used for linear wear
testing on disks on each of 5 patterned oxidized lines.
Figure 2: (Above) Tubular oven used to allow
a continuous airflow to facilitate oxidation.
Figure 4: (Above) Mass lost was measured after
every test with a 5-digit weighing scale.

## Slide 5: Revised Methodology
Only the Ti-6Al-4V alloy disks were used
Polished again up to 600 grit
Masses recorded immediately after each test
Figure 5: (Below) Conventional oven used at 650ºC for 1 hr.
Figure 6: (Above) Four types of tribology tests used.

## Slide 6: Results
Patterns on all four disks created by oxidation were visible
Each placed in the tribometer under four different conditions for 5 minute intervals
Figure 7: (Above left) Progression of Ti-alloy disks. (Clockwise starting from top left) Non-polished, polished to 600 grit, after oxidation, array mask used during oxidation, after tribology.
Figure 8: (Above right) CAD drawing of array mask designed by Carlos R. Ramos-Sáenz.

## Slide 7
Output for tribology tests transferred to Excel where data was processed in a MATLAB program
Trend line is moving average of peak points during tests
  Black: 1mm diameter (1000 microns)
  Orange: 500 microns
  Blue: 250 microns
  Green: 125 microns
  Purple: 35 microns
Figure 9: Demonstration of nanoscaffolds under microscope.

## Slide 8
Chart: Tribology Tests on Ti-6Al-4V Samples Against SS in a Dry Environment
Chart: Tribology Tests on Ti-6Al-4V Samples Against SS in a Lubricated Environment
Chart: Tribology Tests on Ti-6Al-4V Samples Against Bone in a Dry Environment
Chart: Tribology Tests on Ti-6Al-4V Samples Against Bone in a Lubricated Environment

## Slide 9: Mean Mass Gain
Chart: Mean Mass Gain After Oxidation for Ti-6Al-4V Alloy Disks
| TV5 | TV6 | TV7 | TV8 | SS ball, dry | SS ball, Ringer's | bone, dry | bone, Ringer's
Initial | 4.4518 | 4.4148 | 4.2927 | 4.3764
After Oxidation | 4.453 | 4.418 | 4.295 | 4.3783

## Slide 10: Mean Mass Loss
Chart: Mean Mass Loss Of Ti-6Al-4V After Tribology Test Against SS in Dry Envinronment
| After Tribology Test (TT) 1 | After TT 2 | After TT 3 | After TT 4 | Final
 | 4.453 | 4.4529 | 4.4529 | 4.4529 | 4.4529
Chart: Mean Mass Loss Of Ti-6Al-4V After Tribology Test Against SS in Lubricated Envinronment
| After Tribology Test (TT) 1 | After TT 2 | After TT 3 | After TT 4 | Final
 | 4.4171 | 4.4169 | 4.4169 | 4.4169 | 4.4169
Chart: Mean Mass Loss Of Ti-6Al-4V After Tribology Test Against Bone in Lubricated Envinronment
| After Tribology Test (TT) 1 | After TT 2 | After TT 3 | After TT 4 | Final
 | 4.3784 | 4.3784 | 4.3784 | 4.3784 | 4.3784
Chart: Mean Mass Loss Of Ti-6Al-4V After Tribology Test Against Bone in Dry Envinronment
| After Tribology Test (TT) 1 | After TT 2 | After TT 3 | After TT 4 | Final
 | 4.2958 | 4.2958 | 4.2958 | 4.2958 | 4.2958

## Slide 11: Original Tribology Tests of Ti-6Al-4V Alloys
Chart: Tribology Tests for Ti-6Al-4V Alloy Against SS in Dry Environment
Chart: Tribology Tests for Ti-6Al-4V Alloy Against Bone in Dry Environment
Chart: Tribology Tests for Ti-6Al-4V Alloy Against SS in Dry Environment

## Slide 12: Preliminary Conclusions
Most efficient alloy was Ti-6Al-4V alloy in the conventional oven at 650ºC for 1 hr.
Wear was audible and visible, on custom bone pin and alloy disks
Coef. of friction increased when tested against SS in both environments
Lubricated study of bone pin had coef. of friction about 1 compared to dry environment and coef. of friction of about 1.2
For SS, the coef. of friction is dependent on size of scaffold
For bone, there is no dependency for coef. of friction and size of scaffold